Model Specification: 7-DT-4 Steel Dovetail Gratings

October 14, 2021

Specifier Notes: Architect or engineer should carefully review and edit this section to meet the requirements of the project and local building codes. Coordinate this section with other specification sections and the drawings and delete any unused “Specifier Notes” and options shown in red after editing.

This section covers Ohio Gratings, Inc.’s “7-DT-4 Steel Dovetail Pressure Lock Gratings.” Consult Ohio Gratings (www.ohiogratings.com) for assistance in editing this section for specific applications. Call 800.321.9800 or email info@ohiogratings.com with any questions.

SECTION 055300 - Metal Fabrications: Metal Gratings

Part 1: General

1.1 Section Includes

- Prefabricated, custom-designed light-duty steel bar gratings.

- Miscellaneous installation hardware and accessories.

1.2 Reference Standards

- ANSI A326.3-2017: American National Standard Test Method for Measuring Dynamic Coefficient of Friction of Hard Surface Flooring Materials.

- US Department of Justice: Americans with Disabilities Act (ADA) - 2010 Design Standards: Section 302.1: Slip-resistance, and 302.3: Openings.

- ASTM A-1011: CS Type B Steel Strip Hot-Rolled Carbon.

- ANSI/NAAMM MBG 531-17: Metal Bar Grating Manual.

  - Action Submittals

- Product Data: The contractor shall submit the manufacturer’s catalog pages including load tables, anchor details and standard installation details.

- Shop Drawings: The contractor shall submit for approval shop drawings for the fabrication and erection of all gratings, based on construction drawings of current issue. Include plans, elevations, and details of sections and connections as required. Show type and location of all fasteners.

- Samples of grating and anchorage system shall be submitted for approval.

  - Quality Assurance

- Manufacturer Qualification: A company specializing in the manufacture of metal bar gratings with not less than 10 years of documented experience.

- Fabrication tolerances shall be in accordance with applicable provisions and recommendations of ANSI/NAAMM MBG 531-17: Metal Bar Grating Manual.

Part 2: Products

2.1 Source Requirements:

Design is based upon use of gratings as manufactured by Ohio Gratings, Inc. and terminology used herein may include reference to the specific performance or product of this manufacturer. Such reference shall be construed only as establishing the quality of materials, operational features and workmanship used under this section and shall not, in any way, be construed as limiting competition.

2.2 Manufacturers:

Acceptable manufacturers include Ohio Gratings, Inc. (5299 Southway St. SW, Canton, Ohio 44706, 800-321-9800, www.ohiogratings.com) or approved equal.

  - Manufactured Units:

- Description: Carbon Steel Dovetail Pressure Lock Grating type 7-DT-4 with OnGrip® Spray Traction Surface or ALGRIP® Traction Surface. Rectangular bearing bars are slotted to receive slotted rectangular cross bars, which are assembled in egg-crate fashion and hydraulically pressed to permanently lock the bars in place.

- Bearing Bar Spacing: 7/16” on center.

- Bearing Bar Depth: based on loading requirements and clear span.

- Bearing Bar Thickness: 3/16” to provide 1/4” space between bars.

- Cross Bar Spacing: 4” on center.

- Top surface of gratings shall have OnGrip® Spray Traction Surface or ALGRIP® Traction Surface.

- Fabrication:  Fabricate cutouts in grating sections for penetrations as indicated. Arrange cutouts to permit grating removal without disturbing items penetrating gratings. Trim band ends (and cuts in grating) with bars of the same size and material as bearing bars. Include fabrication required for attachment system shown on plans, or as recommended by the manufacturer.

- Design Criteria:

  - Loading: Grating products shall be designed and manufactured to meet live load conditions of 100 lbs. / Sq. Ft with a maximum deflection of 1/4” for the clear spans shown on the drawings. Bearing bar depth shall be as shown on the contract drawings, or as recommended by the manufacturer to meet loading requirements, clear span conditions and maximum deflections specified.

  - Traction / Slip-Resistance: When tested per ANSI A326.3-2017, the top surface shall provide a minimum Wet Dynamic Coefficient of Friction (Wet DCOF) of 0.45 to meet high traction classification. Per ADA Section 302.1, walking surfaces shall provide a slip-resistant surface with sufficient frictional counterforce to the forces exerted in walking to permit safe ambulation.

  - Bearing Bar Orientation:  Per ADA Section 302.3, the gratings shall be oriented with the top surface bearing bars perpendicular to the predominate direction of pedestrian travel.

- Materials: Bearing bars, cross bars and banding shall have mechanical properties equal to, or greater than the performance of carbon steel type ASTM-A-1011 CS Type B.

- Fabrication Tolerances shall be in accordance with ANSI/NAAMM MBG 531-17: Metal Bar Grating Manual.

- Top Surface: OnGrip® Spray Traction Surface or ALGRIP® Traction Surface shall be included in order to meet or exceed Wet Dynamic COF requirements of paragraph 2.3 C.2 above.

- Finish: Gratings shall be Hot-Dip Galvanized per ASTM A-123.

2.4 Accessories:

Provide appropriate fasteners for type, grade, and class required for approved anchorage system.

Part 3: Execution

3.1 Field Verification:

Take field measurements prior to preparation of final shop drawings (and fabrication where required) to ensure proper fitting of the work.

  - Installation

- Prior to grating installation, contractor shall inspect supports for correct alignment and conditions for proper attachment and support of the gratings. Metal shall be used for all grating supports and provide the minimum bearing surface for the depth of grating per ANSI/NAAMM MBG 531-17: Metal Bar Grating Manual. Ends of all bearing bars at cutouts for penetrations are to be supported in like manner. Any inconsistencies between contract drawings and supporting structure deemed detrimental to grating placement shall be reported in writing to the architect or owner’s agent prior to placement.

- Install grating in accordance with shop drawings and standard installation clearances as recommended by ANSI/NAAMM MBG 531-17: Metal Bar Grating Manual.

3.3 Grating Attachment:

Use approved attachment system and fasteners to secure grating to supporting members as shown on plans.